## Slide 1: Special Topics: Water Oxidation Catalysis: Homogeneous or Heterogeneous?
Ulrich Hintermair, Staff Sheehan, Julie Thomsen
Crabtree & Brudvig Labs
Yale Chemistry

## Slide 2: Water Oxidation
Two Half Reactions:
4H+ + 4e− → 2H2 Reduction (lower activation barrier)
2H2O → O2 + 4H+ + 4e− Oxidation (higher activation barrier)
Goal: 2H2O → 2H2 + O2 Water Splitting
Oxidant: CAN ceric ammonium nitrate (high oxidative potential)
NaIO4 Sodium periodate (lower oxidative potential)
Catalyst: IrIII  IrIV
Methods Precipitation Control NP Synthesis Gelation Structure Function Additional Projects
Notes: http://pubs.rsc.org/en/content/articlehtml/2012/cp/c2cp41490b
O-O difficult to form; requires more energy
Low activation barrier means low overpotential
Hydrogen as a clean energy carrier
C-H oxidation instead of water oxidation to obtain target chemicals  reduction reaction is what would make the fuels
Purpose of CH oxidation is for taking C-H to C-O (mainly for specialty chemicals – decalin and THF oxidation)
CH oxidation and reduction in concert – methanol splitting for energy in fuel cells (DMFC)

## Slide 3: Oxidation Catalysis
Platinum: acid stable; not very active
Ruthenium: active; not acid stable
Iridium: active & active stable
Garand E, et. al. Phys Chem Chem Phys 14 10109 (2012).
Methods Precipitation Control NP Synthesis Gelation Structure Function Additional Projects
Notes: Google images “water oxidation catalyst iridium”
Iridium molecular compound with bound chlorine – chloride pops off and gets oxidized also
Periodate grabs electrons – driving force to pull electrons out of iridium; periodate doesn’t get regernerated; gets consumed
Iridium loses 4 electrons to periodate and oxygen from water regernerates the catalyst
Rapidly exchanging weakly bound water; slowest process is OO bond formation ; step before –OOH is rate limiting step; on order of Hz
8 molecules oxygen atom per iridium per second; with dimer catalyst bound to surface (ITO)

## Slide 4: Iridium Precursors
Cp* = pentamethylcyclopentadienyl
Various ligands: tune properties of molecular materials; tune activity
Methods Precipitation Control NP Synthesis Gelation Structure Function Additional Projects
Notes: (in general ligands tune selectivity and mechanism but most importantly here is activity)

## Slide 5: Iridium Catalysis
Blue Solution develops during oxidation reaction
UV-vis measurements
Hintermair U, et. al. JACS 134 9785 (2012).
Methods Precipitation Control NP Synthesis Gelation Structure Function Additional Projects

## Slide 6: Reaction Assessed by Oxygen Generation
Oxygen generated at same time as formation of blue band; oxidant gets consumed
Hintermair U, et. al. JACS 135 10837 (2013).
Methods Precipitation Control NP Synthesis Gelation Structure Function Additional Projects

## Slide 7: If the ligands are stable against oxidation…
No light scattering… no particles…
 Homogeneous catalysis
Hintermair U, et. al. JACS 134 9785 (2012).
Methods Precipitation Control NP Synthesis Gelation Structure Function Additional Projects

## Slide 8: If the ligands are oxidized…
Particles!
 Heterogeneous catalysis
Hintermair U, et. al. JACS 134 9785 (2012).
Methods Precipitation Control NP Synthesis Gelation Structure Function Additional Projects

## Slide 9: Concentration limits growth dynamics
Methods Precipitation Control NP Synthesis Gelation Structure Function Additional Projects
150 equivalents NaIO4
75 equivalents NaIO4
Particle Formation Reaction Kinetics
Notes: First order reaction

## Slide 10: Metal Oxide Particle Synthesis
Aggregation is diffusion controlled
Methods Precipitation Control NP Synthesis Gelation Structure Function Additional Projects
Power law dynamics in aggregate growth

## Slide 11: Diffusion limited aggregation
Particles stick on first contact
In contrast to reaction limited aggregation, where sticking probability < 1 due to reaction energy barrier
Methods Precipitation Control NP Synthesis Gelation Structure Function Additional Projects
Computer simulation
Electrodeposited copper sulfate

## Slide 12: Aggregate Characterization
Over time Df evolves to ~2
Methods Precipitation Control NP Synthesis Gelation Structure Function Additional Projects
Solution only
Suspension forms
Feature at ~30 nm: primary particle size
-2
Notes: Persistent feature at ~30 nm: primary particle size

## Slide 13: “Green” Metal Oxide NP Synthesis
Aqueous, room temperature
Simplest precursor (off-the-shelf)
Methods Precipitation Control NP Synthesis Gelation Structure Function Additional Projects
(in preparation)

## Slide 14: Suspension Stability
Scattered Intensity (magnitude only vs. time)
  Aggregation/sedimentation over time
  Addition of salts/surfactants can affect stability
Growth
Sedimentation
Methods Precipitation Control NP Synthesis Gelation Structure Function Additional Projects