## Slide 1: Environmental Nanomaterial Dynamics: Bridging Length Scales
Sara M. Hashmi, Ph.D.
Director, Facility for Light Scattering
786

## Slide 2: Asphaltenes
Most aromatic component of petroleum fluids
Industrial nuisance
Form pickering emulsions in oil spills
Fracking
water
photonics.com
Particle-stabilized droplets
Stable; difficult to separate
Notes: Pickering emulsions – very stable, difficult to separate

## Slide 3: Asphaltene precipitation
Cascading length scales
Colloid growth & aggregation
photonics.com
π-stack even when stable
Liquid-liquid separation
Sedimentation & deposition
Highly aromatic crude components
nm
µm
A
o
Induced by pressure; temperature; composition
Notes: More aromatics entrained, not heptane for instance

## Slide 4
Nanoparticles
Molecules
Suspensions
Macroscale Flows
Å  nm
nm  μm
mm  cm
mm  cm  m

## Slide 5
Nanoparticles
Molecules
Suspensions
Macroscale Flows
Å  nm
nm  μm
mm  cm
mm  cm  m

## Slide 6: Asphaltene chemistry
Most aromatic; highest MW; may contain metals
Operational definition only:
  Soluble in toluene, aromatic solvents
  Insoluble in heptane, medium chain alkanes
No precise chemical formula
unit.aist.go.jp
Mullins, O. C. Energy & Fuels 24 2179 (2010).
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport
Notes: http://en.wikipedia.org/wiki/Petroleum
unit.aist.go.jp/energy/afg/asphaltene/Chapter1.htm

## Slide 7: Importance of Aromaticity
Alkanes: non-polar
Aromatics: polar
Mixing is unfavorable for large aromatic molecules
Asphaltene
Bound electrons
Delocalized electrons
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport

## Slide 8: Experimental systems: purely organic
  1. Petroleum Fluid: BAB, SB, QAB, M2, CV
  2. Precipitant: heptane
  3. Dispersants: BA, 4F, DBSA
Materials
Mix components, allow precipitation, assess surfactant effects
BAB
SB
QAB
M2
CV
0.841
0.844
0.865
0.867
0.905
0.0031
0.0069
0.0125
0.0351
0.1180
Petroleum fluid ρo (g/mL) f(g/g)
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport
Notes: NOTE: error bars on f and pa very small (10^-5 or less) for QAB and CV

## Slide 9: Surfactant Options
Dodecylbenzenesulfonic acid
DBSA = strong organic acid
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport
BA*
4F*
DBSA
2000
4000
322
Non-ionic
Non-ionic
Anionic
Polyolefin alkeneamine
Alkylated phenol
Known
Name MW Type Molecular Structure
* proprietary (Lubrizol)
Hydrophobic tail
Aromatic ring
Ionic headgroup

## Slide 10: Dissolution by solvent or surfactant
fully dissolved
Toluene: 3 17 30 46 60 80 100 wt. %
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport
Color change indicates chemical reactions
DBSA: 50 250 750 2,500 7,500 10,000 ppm
fully dissolved

## Slide 11: Understanding Molecular Chemistry
c (ppm)
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport
Hashmi, et. al. Soft Matter (2012).
UV-vis spectra
nσ*, nπ* transitions
Ngamna et al. Langmuir 23, 8569-8574 (2007).
Same signature as protonating free electrons in single or double-bonds

## Slide 12: Suggested Protonation Mechanism
Low concentration DBSA
+
Very strong, stable ion pairing in oil
Hashmi, Zhong, Firoozabadi. Soft Matter (2012).
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport

## Slide 13: Suggested Protonation Mechanism
Due to high acidity of DBSA, need to rule out hydrolysis…
Higher concentration DBSA: Solvation shell
Hashmi, Zhong, Firoozabadi. Soft Matter (2012).
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport

## Slide 14: Reversibility of acid-base interactions
~100 mM DBSA + ~100 mM TEA
50,000 ppm = ~100 mM DBSA
TEA competes w/ heteroatomic asphaltene groups to ion-pair w/ DBSA;
triethylamine; pKa~10.7
Removal of non-polar DBSA tails from asphaltenes destabilizes them.
(Ulrich Hintermair, Yale Chemistry)
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport

## Slide 15
Nanoparticles
Molecules
Suspensions
Macroscale Flows
Å  nm
nm  μm
mm  cm
mm  cm  m

## Slide 16: Particle characterization: Light scattering
Incident light
Diffusing particles [nm – μm]
Unperturbed light
Intensity at detector fluctuates due to particle motion  diffusive time scale
Light scatters in all directions
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport
Diffusion constant
Thermal energy scale
Solvent viscosity
Particle size

## Slide 17: Dispersants suppress growth
c (ppm)
Hashmi & Firoozabadi. Energy & Fuels (2012).
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport
Notes: ANIMATE CV χ=600 mL/g

## Slide 18: Dispersants shrink nanoparticles
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport
Size decrease is limited
Similar behavior

## Slide 19: What differentiates surfactants?
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport
Self-association leads to
reverse micelle formation
at critical micelle concentration
Increasing concentration
Measurable via:
conductivity, light scattering, surface tension, viscosity…

## Slide 20: Dispersant critical micelle concentration
by conductivity measurements
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport
BA ~ 10 ppm 4F ~ 100 ppm
Notes: Fix the y axis negative exponents

## Slide 21: Dispersant micellization
by conductivity measurements
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport
BA ~ 10 ppm 4F ~ 100 ppm
Notes: Fix the y axis negative exponents

## Slide 22: Micellization explains the limit
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport
Behavior collapses
But can adsorption alone induce interparticle repulsion?

## Slide 23: In/Stability & interparticle interactions
physics.nyu.edu/~pc86
Universal
Repulsion Required
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport
Brushes: short-ranged
Electrostatics: good candidate to explain stability
However, asphaltene suspensions are non-polar…

## Slide 24: Electrostatics in Non-Polar Systems
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport
Electrostatic attraction is longer range in oil than in water
Double layer indicates range of electrostatic interactions
Aqueous suspensions
Thin double layers
Non-polar suspensions
Thick double layers
-
Notes: https://www.researchgate.net/publication/236186356_Iron_Oxide_Nanoadsorbents_for_Removal_of_Various_Pollutants_from_Wastewater_An_Overview

## Slide 25: Measurement Concept: Zeta Potential
Balance electrostatic force:
+
-
with electric field : diffusion with drift
Electrophoretic mobility:
Drift velocity:
Initial position
Diffusive trajectory
Final position
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport
Against hydrodynamic force:
Related to surface charge:
Surface charge
Notes: Force balance is f=qE=QeE = f=6 pi*eta*a*v  QeE=6pi*eta*a*v  v/E = Qe/6pi*eta*a

## Slide 26: Electrophoretic mobility at c=0 ppm
Hashmi, Firoozabadi. Soft Matter 8, 1878 (2012).
+
+
+
+
-
-
-
-
π electrons
metal ions
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport
Notes: Have checked this over a variety of conditions and several different asphaltene systems – it’s robust! Reason there is nothing near 0 is due simply to the resolution of the instrument

## Slide 27: Dispersant increases surface charge
Hashmi, Firoozabadi. Soft Matter 7, 8384 (2011).
aggregation
stable suspensions
cmc of BA in heptane
CV
QAB
SB
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport

## Slide 28: Adsorption & electrostatic stabilization
Surfactant adsorption on particle surface prevents further growth and aggregation
unstable
stable
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport

## Slide 29
Nanoparticles
Molecules
Suspensions
Macroscale Flows
Å  nm
nm  μm
mm  cm
mm  cm  m

## Slide 30: Controlling Sedimentation in Bulk
t=0 t=3 t=4 t=6 t=100 min
  days or weeks
Hashmi & Firoozabadi J. Phys. Chem. B 114 15780 (2010).
Mix with heptane to induce separation
 FAST separation
GOAL: slow dynamics
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport

## Slide 31: Hard sphere systems: linear front
t = 0 min t = 60 min t = 95 min t = 150 min t = 210 min
1.57 µm radius silica spheres in water at Φ=0.05
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport
Notes: Align pictures – P10805… 37, 52, 59, 641, 572

## Slide 32: Hard sphere systems: linear front
Measured v ~ 2 to 3x slower than expected
Φ
a = 1.57 µm; silica particles in water
Sedimentation Velocity:
µm/s
Silica zeta potential:
ζ = -18.25 +/- 0.31 mV
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport
Density difference
Gravity

## Slide 33: Asphaltene sedimentation dynamics
Adding heptane lowers concentration, slows dynamics
M2; χ =40 (mL/g); c = 0 ppm
t=0 t=3 t=4 t=6 t=100 min
Hashmi & Firoozabadi J. Phys. Chem. B 114 15780 (2010).
Falling, compacting fronts
SB; c = 0 ppm
χ (mL/g)
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport

## Slide 34: Gelling systems: sudden collapse
Lietor-Santos et. al. Langmuir. 26(5), 3174 (2010).
Poon et. al. Faraday Discuss. 112, 143 (1999).
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport

## Slide 35: Sedimentation of unstable particles
NP formation
Aggregation
FAST Sedimentation
FAST
Separation
Sedimentation speed ~ (aggregate size)2
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport

## Slide 36: Dispersants slow sedimentation
c (ppm)
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport
Collapsing front disappears
Hashmi & Firoozabadi J. Phys. Chem. B 114 15780 (2010).

## Slide 37: Stable particles slow aggregation
NP formation
Aggregation
SLOW Sedimentation
SLOW Separation
Sedimentation speed ~ (aggregate size)2
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport

## Slide 38
Nanoparticles
Molecules
Suspensions
Macroscale Flows
Å  nm
nm  μm
mm  cm
mm  cm  m

## Slide 39: Application: Address Clogging
cm
cm
mL
Transducer
L >> R
Nozzle for mixing
Mix with heptane to precipitate:
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport
Pressure drop
Flow rate
Pipe Flow:
Notes: Viscosity = 33 cP; phi ~ 10% by weight

## Slide 40: Convection-Diffusion
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport
Diffusive boundary layer: particles within the layer are prone to stick; particles beyond continue flowing
R
R0
Deposition constricts pipe: requires higher pressure
Hashmi et. al. Physics of Fluids (2015).

## Slide 41: Dispersants reduce deposition
Mixture C; Q = 4.2 mL/hr; Pipe 1;
Each trace is average of 5 runs
c (ppm)
Parameter: changing particle size
“Inhibition”
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport
Notes: WHERE IS THE DATA PLOT SHOWING DECREASED DEPOSITION WITH BOTH BA AND DBSA???

## Slide 42: Dispersants reduce deposition
More dispersant (c)  smaller particles  less clogging (ΔP)!
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport
Notes: WHERE IS THE DATA PLOT SHOWING DECREASED DEPOSITION WITH BOTH BA AND DBSA???

## Slide 43: Dispersants reduce deposition
Without dispersant
With dispersant
Charge-stabilized colloids flow rather than stick
Destabilized asphaltenes deposit on the metal pipe
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport
Some degree of prevention…Can we remove the deposit…?
Notes: WHERE IS THE DATA PLOT SHOWING DECREASED DEPOSITION WITH BOTH BA AND DBSA???

## Slide 44: Deposition Run Followed by Removal
Deposition run: Mixture C
Time = 0 signifies start of removal run
Example: removal run is CVA with DBSA
Impedance mismatch:
change between deposition & removal
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport

## Slide 45: Removal by 5% DBSA in CVA
Fastest flow rate seems most effective: shear effects
Q (mL/min)
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport

## Slide 46: Comparison DBSA & toluene
5% DBSA as effective as 50% toluene!
composition
Removal at < 0.2 PV suggests
Molecular Assembly Nanoparticle Interactions Bulk Sedimentation Deposition & Transport
Hashmi et. al. SPE Journal (2015).

## Slide 47: Importance of the nanoscale
+
+
+
+
+
+
+
+
+
+
Stabilizing
repulsion
Microscopic
instability
Bulk sedimentation: controlled by
Nanoparticle stability: in turn controlled by
Molecular considerations
Visible
Separation
controlled by

## Slide 48: Conclusions
Strong organic acid creates molecular assemblies with asphaltenes
Non-ionic (proprietary) surfactants adsorb to asphaltenes, facilitate electrostatic colloidal stabilization
Macroscopic deposition & sedimentation can be controlled by understanding surfactant mechanisms employed on molecular & colloidal scale
+
+
+
+
+
+
+
+
+
+
Stabilizing
repulsion

## Slide 49: Acknowledgments
Abbas Firoozabadi, Yale/RERI
Michael Loewenberg, Yale
Menachem Elimelech, Yale
Eric Dufresne, ETH Zurich
Ian Morrison, Harvard
Sven Behrens, GA Tech
Ulrich Hintermair, Bath
May 2009
Chevron ~ Maersk ~ ADCO ~ Pemex ~ Lubrizol
Undergraduate Assistants
Leah Quintiliano, Kathy Zhong, Salvatore DeLucia, John Wolff, Batsi Swiswa, Hua Wang, Anjali Khetan