## Slide 1: Static Light Scattering Part 1: Aggregate Structure & Internal Dynamics
786

## Slide 2: Understanding SLS ‘static’ data
I(q): control parameter q [units 1/Length]
Large q probes small length scales
Small q probes large length scales
Shape of I vs q reveals particle structure

## Slide 3: What can light scattering measure?
Molar mass, M
Size, rg
Second virial coefficient, A2
Translational diffusion coefficient, DT
  - Can be used to calculate rh
For a solute in solution, light scattering can determine:
Notes: Notes: With the controlled parameters of an experiment, it is possible with a light scattering measurement to retrieve the molar mass (M), size (rg), second virial coefficient (A2), and translational diffusion coefficient (DT) of a solute in solution. One of the tremendous advantages of light scattering over almost any other method is that these properties can be measured in solution in a non-invasive manner.
Depending on the type of experiment, a light scattering measurement retrieves different aspects of the above-mentioned properties. For example, in an unfractionated sample, or a batch measurement, the measured molar mass is averaged over the weight distribution of the sample, while the size determined in such a measurement is an average over the radius squared. For fractionated samples, the unaveraged mass and size distributions can be obtained, and from this, information about conformation can be determined.
Also, the first three quantities, M, rg, and A2, are measured via a technique called either classical, static, or Rayleigh scattering. In this technique, the time scale of the measurement is long compared to rapid fluctuations in scattered intensity due to molecular motion. These fluctuations are hence averaged out. The focus of today’s lecture is Rayleigh scattering. It is also possible to measure the fast (nanosecond) fluctuations of the scattered intensity in a technique known as dynamic light scattering, photon correlation spectroscopy, or Quasi-Elastic Light Scattering (QELS). This type of measurement determines the translational diffusion coefficient for the solute, which is sometimes converted to an effective hydrodynamic radius (rh) based on the assumption that the solute is a sphere.

## Slide 4: Understanding SLS ‘static’ data
Very small particles scatter isotropically
I(q) ~ constant
Larger aggregates can be assessed for their fractal dimension Df, in region where I ~ q-Df
rusnauka.com
Notes: http://www.rusnauka.com/46_PWMN_2015/Tecnic/6_205010.doc.htm

## Slide 5: Dimensionality
From linear dimension to areal dimension, non-fractal linear objects are squared to give area
From linear dimension to volume dimension, non-fractal linear objects are cubed to give volume
Fractal objects: can’t obtain area simply by squaring linear portion, nor volume simply by cubing linear segment

## Slide 6: Fractal Dimensions
1 dimensional object
2 dimensional object
3 dimensional object
Df > 1
Df approaching 2
Df > 1
Df approaching 2

## Slide 7: Example: CNT dispersions
CNT dispersions reveal fractal aggregates
Fractal region may not extend over entire q range
Remember: Large q probes small length scales; Small q probes large length scales

## Slide 8: Example: Fullerene NP aggregation
Aggregate growth extends range of q in the power law region

## Slide 9: Df ~ 1? …Correction to Stokes for Rods
DLS measures Diffusion constant D 
Spheres:
Rods with length L diameter d:
van Bruggen, Lekkerkerker, Dhont, Physical Review E (1997) 56 4394.
Brancaa, Magazu, Mangione. Diamond & Related Materials (2005) 14 846.

## Slide 10: Dependence on Aspect Ratio
p = D/L;
Legend indicates values of L (nm)
Both bundling & length increase diffusion time τ as a function of aspect ratio p

## Slide 11: Also: dynamics as a function of angle
SLS can simultaneously measure angular dependence of dynamics in the system
Diffusive dynamics are defined by 2 quantities:
  control parameter wave vector q [units 1/Length]
  measured time scale τ
Diffusion has units [L2/T] D = 1/q2τ
We can measure τ vs q. If D is constant, we expect…

## Slide 12: Fluctuation time-scale τ vs. q
Typical diffusive behavior should exhibit a power law with slope -2
-2
If D is a constant, then
D = 1/q2τ
and so
τ = (1/D) q-2

## Slide 13: Fluctuation time-scale τ vs. q
Dynamics in Combo evolve over time. The ‘kinks’ in the dynamics at higher q, beginning at 1/q ~ 75 nm, are robust!
Typical diffusive behavior should exhibit a power law with slope -2
-2

## Slide 14: Investigating Morphology
Transition at 1/q ~ 75 nm in both structure and dynamics
may suggests spherical ‘primary particles’ at sizes <75 nm.
DYNAMICS
STRUCTURE
Power law region indicates fractal structure, Df < 3.

## Slide 15: Lab tasks
SLS on CNT samples
SLS on protein/polymer/gel samples
More to come on SLS…