## Slide 1: Recap of Day 1
786

## Slide 2: Concepts & Lab
Introduction to Dynamic Light Scattering
  Measurement of diffusive time scales via intensity fluctuations
  Data fitting options
  Practical considerations
  (Slides now online? With )
Measurement of DI water, PS latex spheres & ‘mystery sample’

## Slide 3: PS Latex standards
1000x dilution from stock
Nominal 50nm & 200nm diameter individually
  Cumulant results: 3 measures of radius within 1%
  PDI values less than 0.05
  Very mono-dispersed “well-behaved” samples

## Slide 4: 1:1 Mixture
Appearance of single decay and single peak in size distribution
Size ratio: 115nm / 30nm = factor of 3.8
  Possibly not sufficiently well-separated
Measurement at 150 degrees did not resolve
  30nm no longer scattering isotropically
Other options
  Would CONTIN analysis resolve peaks?
  What if small particles were predominant with only fraction of large ones?